Romolo Multi Plus Tile Adhesive Powder is a mineral-based product that offers strong adhesion and ease of use for installation on various surfaces. It is designed with waterproof compounds and ionization technology, making it suitable for applications like pools, water tanks, saunas, jacuzzis, and elevated slab stone installations. This adhesive powder reduces the dead load of the building and can be used on different types of surfaces.

**Specifications:**

Fast adhesion and drying

Low cost and easy installation

Suitable for use in all climates

Capaballity of use in high altitudes

Strong adhesion to all building materials

High resistance to moisture, steam, acid, and petroleum

Superior flexibility preventing cracks or detachment of tiles or stones

Rapid drying and efficient rigidity, enabling fast preparation and performance

**Applications:**

Usable for water tanks

Usable for pools, saunas, and jacuzzi

Can be installed on tiles, glass , clay surfaces

Can be installed on panels, and wood surfaces

Can be applied to plaster surfaces, cement surfaces

Can be installed on concrete surfaces, prefabricated parts

Usable for porcelain ceramic installations on floors, walls, and elevations

Suitable for both indoor and outdoor installations of different stone slabs

Ideal for various materials such as tiles, ceramics, antique stones, and plastic stones

**How to use:**

To summarize, before applying the Romolo Multi Plus Tile Adhesive Powder, it is important to clean the surface and create a scratch for better adhesion. The recommended ratio is 4 kg of glue mixed with 1 liter of water. Thoroughly mix the adhesive before applying it behind the tile and at the desired level. The consumption rate is generally 4-5 kg per square meter.

**Attention:**

The suitable temperature range for using the adhesive is 5-40°C. This adhesive has high adhesion due to its low water absorption and should be used within 7-10 minutes after mixing with water.

**Packaging:**

Romolo Multi Plus Tile Adhesive Powder is conveniently offered in 20kg bags for your ease of use and preference.

**Storage:**

The recommended temperature range for storing the product is between 10-30°C. The product has a shelf life of 9 months when kept in its original, unopened packaging. It is important to store it away from direct sunlight, extreme cold, heat, and frost to maintain its quality and effectiveness.

**Safety:**

To ensure safety, it is advised to avoid direct contact with the eyes and skin. It is recommended to wear gloves and protective glasses when handling the product. In the event of accidental contact with the eyes, it is crucial to immediately rinse them with lukewarm water for a minimum of 15 minutes.

**Temprature:**

The suitable working temperature is between 5 to 40 degrees Celsius, the drying time varies between 12 to 72 hours depending on the weather conditions.